| Applicant: | Xihe (Ningbo) Fashion Technology Co., Ltd. |
| --- | --- |
| Address: | 3rd Floor, Block B, Hengyu Center, No. 200th Kechuang North Road, Haishu District, Ningbo City, Zhejiang Province, China |
| Contact Person: | Annie |

| Sample Description: | Shell fabric |  |  |
| --- | --- | --- | --- |
| Collection: | YOGURT COLLECTION | Colour: | 50 PASTEL BLUE |
| Season: | Spring-summer 26 | Fabric Content: |  |
| End Use: | TOP/trousers | Manufacturer: | - |
| Ref No.: | 37052530/37082529 | Order No. | 4800888948/4500888949/ 4500888946/4500888947 |
| Style No.: | 300604MP TOP YOGURT/ 300605MP Trousers | Buyer: |  |
| Testing Stage: | Bulk | Retest-Previous Report No.: | - |
| Package Test: | Individual Test Items |  |  |

| Care Instruction: |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |

| Receipt Date of Sample: | Received on 2026-03-31 |
| --- | --- |
| Date of Testing: | From 2026-03-31 to 2026-04-03 |
| Sample Submitted: | The sample(s) and its (their) information was (were) submitted by applicant and identified. |
| Test Result: | Refer to next page. |

| TÜV SÜD Certification and Testing (China) Co., Ltd. Ningbo Branch |  |
| --- | --- |
| Prepared by: | Authorized by: |
| ________________ Kiki Lu Softlines Department | _____________________ Debra Cui Softlines Department |

| Description of The Test Subject |  |  |
| --- | --- | --- |
| Sample | Description | Photo |
|  | 63% viscose 37% linen woven fabric in 50 PASTEL BLUE |  |

| Conclusion |  |  |  |
| --- | --- | --- | --- |
| Test Items |  | Test Component | Conclusion |
| Individual Test Items |  |  |  |
|  | Determination of the slippage resistance of yarns at a seam in woven fabrics | A | Pass |
|  | Dimensional Change after washing | A | Fail |
|  | Colour Fastness to light | A | Fail |

| Remarks: | Pass = Meet Client’s Requirement | Fail = Below Client’s Requirement |
| --- | --- | --- |
|  | * = No Specified Requirement | # = No Comments |
|  | N/A = Not Applicable | - = Not Conducted |

|  | TEST RESULTS |
| --- | --- |

| 1 | Determination of the slippage resistance of yarns at a seam in woven fabrics |  |  |
| --- | --- | --- | --- |
|  | ISO 13936-1:2004 |  |  |
|  | Slippage At 6mm | A | Client’s Requirement |
|  | Seam//Warp (N) | >200 | ≥150N |
|  | Seam//Weft (N) | >200 | ≥150N |

| 2 | Dimensional Change after washing |  |  |
| --- | --- | --- | --- |
|  | ISO 5077:2007/ISO 3759:2011/ISO 6330:2021; Procedure No.:3M; Using horizontal axis, front-loading type machine: Machine wash at 30°C with 2 kg Total dry mass and ECE(A) detergent +TAED+ sodium perborate, line dry. |  |  |
|  | After 1 Wash | A | Client’s Requirement |
|  | Lengthwise (%) | -7.1 | ±3% |
|  | Widthwise (%) | -1.4 | ±3% |

|  | Remarks: | (+) Means Extension; (-) Means Shrinkage |
| --- | --- | --- |

| 3 | Colour Fastness to light |  |  |
| --- | --- | --- | --- |
|  | ISO 105-B02:2014; Use Water Cooled Xenon Arc Lamp |  |  |
|  | Up to Grade 5 | A | Client’s Requirement |
|  | Grade(blue wool standard) | 4 | ≥5 |

|  | -End of The Test Report- |
| --- | --- |