| Abrasion Resistance-Rotating Drum Method |  |  | ISO 4649:2024 Method B(Rotation test) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Report No: | 87.441.26.1919830.01 |  |  | Date In: |  |  |  |
| Sample Ref: | 001 |  |  | Date Out: |  |  |  |
| Sample Description: |  |  |  |  |  |  |  |
| 1.Condition: | 23 ± 2°C / 50 ± 2% RH × 16 hours(recommend 16 hours) |  |  |  |  |  |  |
| 2.Test atmosphere: | 23 ± 2°C / 50 ± 2% RH |  |  |  |  |  |  |
| 3.Test Result: | The Method of Cleaning: a brush attached to a vacuum cleaner |  |  |  |  |  |  |
| Sample | Results |  |  |  | Requirement |  | Conclusion |
| 001 | Density(g/cm³) | 3.25 |  |  |  |  |  |
| 001 | Relative Volume Loss(mm³) | 153.5 |  |  | ≤ 300 |  | PASS |
| 001 | Abrasion resistance Index | 113.33 |  |  |  |  |  |
| Remark: |  |  |  |  |  |  |  |

END OF REPORT RESULT

| 4.Calculation: |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Density of test Sample: |  |  |  |  |  |  |  | ρ= ρwm1m1-m2 |
| Specimen A: | 1.3000 × 1.0g/cm³ / (1.3000 - 0.9000) |  |  |  |  | 3.2500 | g/cm³ |  |
| Specimen B: | 1.3000 × 1.0g/cm³ / (1.3000 - 0.9000) |  |  |  |  | 3.2500 | g/cm³ |  |
| Ave: |  |  |  |  |  | 3.25 | g/cm³ |  |
| [Abrasion distance: |  | full |  |  | the abrasion distance] |  |  |  |
| Specimen 1: | 1000 × (2.3000 - 1.8000) × 400mg / [3.25 × (200.0000 + 201.0000)] |  |  |  |  | 153.462 | mm³ | ∆Vrel=∆mt∆mconstρt∆mr |
| Specimen 2: | 1000 × (2.3000 - 1.8000) × 400mg / [3.25 × (200.0000 + 201.0000)] |  |  |  |  | 153.462 | mm³ |  |
| Specimen 3: | 1000 × (2.3000 - 1.8000) × 400mg / [3.25 × (200.0000 + 201.0000)] |  |  |  |  | 153.462 | mm³ |  |
| Ave: |  |  |  |  |  | 153.5 | mm³ |  |
| Density of reference compound: |  |  |  |  |  |  |  |  |
| Specimen A: |  |  |  |  |  |  |  |  |
| Specimen B: |  |  |  |  |  |  |  |  |
| Ave: |  |  |  |  |  |  |  |  |
| Abrasion resistance Index: |  |  |  |  |  |  |  |  |
| Specimen 1: | ((200.0000 + 201.0000) / 2 × 3.25) / (0.5000 × 1000 × 1.15) × 100 |  |  |  |  | 113.33 |  | IAR= ∆mrρt∆mtρr ×100 |
| Specimen 2: | ((200.0000 + 201.0000) / 2 × 3.25) / (0.5000 × 1000 × 1.15) × 100 |  |  |  |  | 113.33 |  |  |
| Specimen 3: | ((200.0000 + 201.0000) / 2 × 3.25) / (0.5000 × 1000 × 1.15) × 100 |  |  |  |  | 113.33 |  |  |
| Ave: |  |  |  |  |  | 113.33 |  |  |

Equipment No: SFL-NGB-FWEQP- 002,003