| Test Report Number | 87.405.26.15535.01 |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Basic Info |  |  |  |  |  |
| Reviewer: |  | Cutting: | NB Lab ECD: | Barcode: |  |
| Sample Description |  |  |  |  |  |

| Index | Test Item | Test Method | Test Param | Sample | Cutting Method | Requirement |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Determination of Dimensional Change in Washing(水洗尺寸稳定性) | ISO 6330:2021, ISO 3759:2011, ISO 5077:2007 | [A]: SpecialCareInstruction: Front zippers must be opened, wash inside out ReferenceDetergents: Reference Detergents 3 WashProcedure: 3N ReferenceDetergentsComposition: 77% ECE(A)+3% TAED+20% Sodium Perborate DryProcedure: Line Dry MachineType: Type A WashingTemperature: 30 WashLoad: 2 BallastType: Type III (100% Polyester) ReferenceDetergentsDosage: 20g WashCycle: 1 IronProcedure: / | A | SpecimenArea=500mm×500mm | "-3%" < "ShrinkageAvg" < "3%" |
| 2 | Colour Fastness to Washing(水洗色牢度测试) | ISO 105-C06:2010 | [A]: TestNo: ref A2S WashingTemperature: 30 BallNumber: 0 BallType: Steel Detergent: ECE(B) Multi-fibre: DW | A | SpecimenArea=40 mm × 100 mm | "GreyScaleChange" ≥ "3" |